## Slide 1: BOSTIK 3070
VISKOPLASTIČNO PLUTO
PREDNOSTI |  | 
Brzo sušenje vrlo dobra izolacija protiv buke, topline i hladnoće |  | 
OPIS PROIZVODA Prikladno za zvučnu i toplinsku izolaciju na okvirima prozora do zida, na okvirima vrata i na pregradnim zidovima te za druge moguće primjene zvučne i toplinske izolacije. BOSTIK 3070 je visokokvalitetna brtva za zvučnu i toplinsku izolaciju. Materijal se sastoji od granula pluta i elastičnog veziva, tvoreći viskoplatično jednokomponentno brtvilo. Stanice pluta ispunjene zrakom daju BOSTIK 3070 odlična zvučna i toplinsko izolacijska svojstva. Zvučna izolacija DIN 52210 (IPB-GS 133/90) potvrda o ispitivanju "Fraunhoferovog instituta za strukturnu fiziku" Stuttgart, uz MPA u Dortmundu (Potvrda o ispitivanju 231426392) protupožarno ponašanje klasa građevinskog materijala DIN 4102 - B 2. Rezultati mjerenja sa zajedničkom dimenzijom 1950 x 10 x 110 mm (izvadak iz izvješća o ispitivanju od Institut Fraunhofer): |  | 
Sastav | granule pluta povezane ljepilom
Boja | pluto
Specifična težina | 0,35 g/cm³
Konzistencija | Čvrsta plastika, stabilna, može se obraditi pištoljem (pod pritiskom) ili ručno
Otpornost na temperaturu | -30 do 1200C
Sušenje | otprilike 6 do 12 sati, ovisno o temperaturnim uvjetima
Za izolaciju | zvuka, topline i hladnoće
Zvučna izolacija | 27 dB na prazan spoj i 30 dB u kombinaciji sa trajno lastičnom brtvom
Primjena | zračni pištolj ili brtva
Temperatura primjene | + 5 °C to + 40 °C
Čišćenje | Bostik Solvent 270, Bostik Solvent 250
KARAKTERISTIKE PROIZVODA
PRIMJENA
Izrada fuga | R ST, W (izolacija spojeva)
Prazna fuga | 19 dB
Sa mineralnim vlaknima | 37 dB
Sa BOSTIK 3070 | 46 dB
Sa brtva BOSTIK 3070 približno 3 mm i trajno elastično brtvilo za fuge na jednoj strani (nakon 3 tjedna vulkanizacije) | 49 dB
Maksimalna moguća izolacija | 50 dB

## Slide 2
 |  | 500 g duguljasta vrećica. U nekim slučajevima izolacijski materijal BOSTIK 3070 može dugo mirisati poput gumene otopine
Ljepljene površine moraju biti suhe i bez masnoće. Vrijeme odzračivanja je najmanje 30 minuta, a najviše 24 h. Primjena BOSTIK 3070 moguća je sa pištoljem na komprimirani zrak ili ručno. Pripremljene spojeve treba ravnomjerno ispuniti BOSTIK 3070. SKLADIŠTENJE Čuvati na hladnom i suhom mjestu, 12 mjeseci. |  | 
SAFETY
For more details, consult the safety data sheet on https://bostiksds.thewercs.com/default.aspx
The information given and recommendations made herein are based on Bostik’s research only and are not guaranteed to be accurate. The performance of the product, its shelf life, and application characteristics will depend on many variables, including the kind of materials to which the product will be applied, the environment in which the product is stored or applied, and the equipment used for application. Any change in any of these variables can affect the product’s performance. It is the buyer’s obligation, prior to using the product, to test the suitability of the product for an intended use under the conditions that will exist at the time of the intended use. Bostik does not warrant the product’s suitability for any particular application. The product is sold pursuant to Bostik’s Terms and Conditions of Sale that accompanies the product at the time of sale. Nothing contained herein shall be construed to imply the nonexistence of any relevant patents or to constitute permission, inducement, or recommendation to practice any invention covered by any patent, without authority from the owner of the pat
PRIPREMA PODLOGE
PAKIRANJE
NAPOMENE